| TYPE | LOAD BAR SIZE | CROSS BAR | WEIGHT (KG/M2) |  | 300 SPAN/mm | 400 SPAN/mm | 500 SPAN/mm | 600 SPAN/mm | 700 SPAN/mm | 800 SPAN/mm | 900 SPAN/mm | 1000 SPAN/mm | 1100 SPAN/mm | 1200 SPAN/mm | 1300 SPAN/mm | 1400 SPAN/mm | 1500 SPAN/mm | 1600 SPAN/mm | 1700 SPAN/mm | 1800 SPAN/mm | 1900 SPAN/mm | 2000 SPAN/mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| GA203/33/33G | 20x3 | 10X2 | 21.6 | U D | 77.2 0.66 | 43.4 1.18 | 27.8 1.84 | 19.3 2.66 | 14.2 3.64 | 10.8 4.77 | 8.6 6.07 | 6.9 7.54 | 5.7 9.18 | 4.8 10.99 | 4.1 13.00 | 3.5 15.20 | 3.1 17.59 | 2.7 20.20 | 2.4 23.02 | 2.1 26.06 | 1.9 29.34 | 1.7 32.87 |
| GA205/33/33G | 20x5 | 10X3 | 35.0 | U D | 128.6 0.66 | 72.3 1.17 | 46.3 1.84 | 32.1 2.66 | 23.6 3.63 | 18.1 4.77 | 14.3 6.06 | 11.6 7.53 | 9.6 9.17 | 8.0 10.98 | 6.8 12.98 | 5.9 15.17 | 5.1 17.56 | 4.5 20.16 | 4.0 22.97 | 3.6 26.00 | 3.2 29.26 | 2.9 32.77 |
| GA253/33/33G | 25x3 | 10X2 | 25.7 | U D | 120.6 0.53 | 67.8 0.94 | 43.4 1.47 | 30.1 2.12 | 22.1 2.90 | 17.0 3.80 | 13.4 4.83 | 10.9 5.98 | 9.0 7.28 | 7.5 8.71 | 6.4 10.28 | 5.5 11.99 | 4.8 13.86 | 4.2 15.87 | 3.8 18.05 | 3.3 20.40 | 3.0 22.91 | 2.7 25.60 |
| GA255/33/33G | 25x5 | 12X3 | 43.4 | U D | 200.9 0.53 | 113.0 0.94 | 72.3 1.47 | 50.2 2.12 | 36.9 2.90 | 28.3 3.80 | 22.3 4.83 | 18.1 5.99 | 14.9 7.28 | 12.6 8.71 | 10.7 10.28 | 9.2 12.00 | 8.0 13.86 | 7.1 15.89 | 6.3 18.07 | 5.6 20.42 | 5.0 22.93 | 4.5 25.63 |
| GA303/33/33G | 30x3 | 10X2 | 39.57 | U D | 173.6 0.44 | 97.6 0.78 | 62.5 1.22 | 43.4 1.77 | 31.9 2.41 | 24.4 3.16 | 19.3 4.01 | 15.6 4.97 | 12.9 6.03 | 10.9 7.21 | 9.2 8.50 | 8.0 9.91 | 6.9 11.43 | 6.1 13.08 | 5.4 14.86 | 4.8 16.76 | 4.3 18.80 | 3.9 20.98 |
| GA305/33/33G | 30x5 | 12X3 | 50.3 | U D | 289.3 0.44 | 162.7 0.78 | 104.2 1.22 | 72.3 1.77 | 53.1 2.41 | 40.7 3.16 | 32.1 4.01 | 26.0 4.97 | 21.5 6.03 | 18.1 7.21 | 15.4 8.50 | 13.3 9.91 | 11.6 11.44 | 10.2 13.09 | 9.0 14.87 | 8.0 16.77 | 7.2 18.81 | 6.5 20.99 |
| GA323/33/33G | 32x3 | 10X2 | 31.5 | U D | 197.52 0.41 | 111.10 0.73 | 71.11 1.15 | 49.38 1.65 | 36.28 2.26 | 27.78 2.96 | 21.95 3.75 | 17.78 4.65 | 14.69 5.65 | 12.34 6.75 | 10.52 7.95 | 9.07 9.26 | 7.90 10.69 | 6.94 12.22 | 6.15 13.88 | 5.49 15.65 | 4.92 17.54 | 4.44 19.56 |
| GA325/33/33G | 32x5 | 12X3 | 53.0 | U D | 329.2 0.41 | 185.2 0.73 | 118.5 1.15 | 82.3 1.65 | 60.5 2.26 | 46.3 2.96 | 36.6 3.75 | 29.6 4.65 | 24.5 5.65 | 20.6 6.75 | 17.5 7.95 | 15.1 9.27 | 13.2 10.69 | 11.6 12.23 | 10.3 13.88 | 9.1 15.66 | 8.2 17.55 | 7.4 19.58 |
| GA353/33/33G | 35x3 | 10X2 | 34.0 | U D | 236.3 0.38 | 132.9 0.67 | 85.1 1.05 | 59.1 1.51 | 43.4 2.06 | 33.2 2.70 | 26.3 3.43 | 21.3 4.24 | 17.6 5.15 | 14.8 6.15 | 12.6 7.25 | 10.9 8.44 | 9.5 9.73 | 8.3 11.13 | 7.4 12.63 | 6.6 14.23 | 5.9 15.94 | 5.3 17.77 |
| GA355/33/33G | 35x5 | 12X3 | 57.1 | U D | 393.8 0.38 | 221.5 0.67 | 141.8 1.05 | 98.5 1.51 | 72.3 2.06 | 55.4 2.70 | 43.8 3.43 | 35.4 4.24 | 29.3 5.15 | 24.6 6.15 | 21.0 7.25 | 18.1 8.44 | 15.8 9.74 | 13.8 11.13 | 12.3 12.63 | 10.9 14.24 | 9.8 15.95 | 8.9 17.78 |
| GA403/33/33G | 40x3 | 10X2 | 38.1 | U D | 308.6 0.33 | 173.6 0.59 | 111.1 0.92 | 77.2 1.32 | 56.7 1.80 | 43.4 2.36 | 34.3 2.99 | 27.8 3.70 | 23.0 4.49 | 19.3 5.37 | 16.4 6.32 | 14.2 7.35 | 12.3 8.48 | 10.8 9.68 | 9.6 10.98 | 8.6 12.37 | 7.7 13.84 | 6.9 15.42 |
| GA405/33/33G | 40x5 | 12X3 | 64.0 | U D | 514.4 0.33 | 289.3 0.59 | 185.2 0.92 | 128.6 1.32 | 94.5 1.80 | 72.3 2.36 | 57.2 2.99 | 46.3 3.70 | 38.3 4.50 | 32.1 5.37 | 27.4 6.32 | 23.6 7.36 | 20.6 8.48 | 18.1 9.69 | 16.0 10.98 | 14.3 12.37 | 12.8 13.85 | 11.6 15.42 |
| GA453/33/33G | 45x3 | 10X2 | 42.2 | U D | 390.6 0.29 | 219.7 0.52 | 140.6 0.81 | 97.6 1.17 | 71.7 1.60 | 54.9 2.09 | 43.4 2.66 | 35.2 3.29 | 29.1 3.99 | 24.4 4.76 | 20.8 5.60 | 17.9 6.52 | 15.6 7.51 | 13.7 8.57 | 12.2 9.71 | 10.9 10.93 | 9.7 12.23 | 8.8 13.62 |
| GA455/33/33G | 45x5 | 12X3 | 70.9 | U D | 651.0 0.29 | 366.2 0.52 | 234.4 0.81 | 162.7 1.17 | 119.6 1.60 | 91.5 2.09 | 72.3 2.66 | 58.6 3.29 | 48.4 3.99 | 40.7 4.76 | 34.7 5.60 | 29.9 6.52 | 26.0 7.51 | 22.9 8.57 | 20.3 9.71 | 18.1 10.94 | 16.2 12.24 | 14.6 13.62 |
| GA503/33/33G | 50x3 | 10X2 | 46.4 | U D | 482.2 0.26 | 271.2 0.47 | 173.6 0.73 | 120.6 1.06 | 88.6 1.44 | 67.8 1.88 | 53.6 2.39 | 43.4 2.95 | 35.9 3.58 | 30.1 4.27 | 25.7 5.03 | 22.1 5.85 | 19.3 6.74 | 17.0 7.69 | 15.0 8.71 | 13.4 9.80 | 12.0 10.96 | 10.9 12.19 |
| GA505/33/33G | 50x5 | 12X3 | 87.5 | U D | 803.7 0.26 | 452.1 0.47 | 289.3 0.73 | 200.9 1.06 | 147.6 1.44 | 113.0 1.88 | 89.3 2.39 | 72.3 2.95 | 59.8 3.58 | 50.2 4.27 | 42.8 5.03 | 36.9 5.85 | 32.1 6.74 | 28.3 7.69 | 25.0 8.71 | 22.3 9.80 | 20.0 10.96 | 18.1 12.20 |
| GA605/33/33G | 60x5 | 12X3 | 91.4 | U D | 1157.3 0.22 | 651.0 0.39 | 416.6 0.61 | 289.3 0.88 | 212.6 1.20 | 162.7 1.57 | 128.6 1.99 | 104.2 2.46 | 86.1 2.98 | 72.3 3.55 | 61.6 4.18 | 53.1 4.86 | 46.3 5.59 | 40.7 6.38 | 36.0 7.22 | 32.1 8.12 | 28.9 9.07 | 26.0 10.09 |
| GA655/33/33G | 65x5 | 12X3 | 98.3 | U D | 1358.3 0.20 | 764.0 0.36 | 489.0 0.56 | 339.6 0.81 | 249.5 1.11 | 191.0 1.45 | 150.9 1.83 | 122.2 2.27 | 101.0 2.75 | 84.9 3.28 | 72.3 3.85 | 62.4 4.48 | 54.3 5.15 | 47.8 5.87 | 42.3 6.65 | 37.7 7.48 | 33.9 8.35 | 30.6 9.28 |

- Spans to the left of the heavy line have a deflection of less than 4mm for a 4kPa uniformly distributed lad.

- The weights shown above include zinc coating and banding for load bar over 1m (the weight of rubber infill only on those highlighted in green).

- The codes in green are ones we stock and includes the rubber infill and flat bar weight in the weight (kg/m2)

- U=Safety Uniformity Distributed Load Bar, Kpa.

- D=Deflection in mm.

- The Load Bar Sheet is calculated based on Pitch of 33.3mm. Other dimensions are also available.

- The Spans above are for easy referencing. There is no size limit for grating length selection

  - Uniformity Distributed Load Bar, KN/m2

  - Load Bar Pitch=33.3mm

  - Allowable Stress = 1.4 x 104  KN/m2

# Text boxes

### GRATEART LOAD AND DEFLECTION TABLE